## Slide 1: Making Invisi-Slip Device

## Slide 2
Make Mold
Spin 100um PDMS, partial cure.
Add FEP window with grease on underside
Lay Block on top with grease on underside
Coat until about 2.3mm in total height
Punch ports both ends 1.5mm punch
Remove from mold and remove plastic piece and wash in Hexane to remove grease

## Slide 3: General Constraints